302 – FAMILY TENT

- Usage:

Special design for relief usage, providing shelter for a family size

- Purpose

It is recognized that tents are not always the shelter solution of choice, but there are many occasions when they are required. In this practical context, it is important that those that are deployed are well adapted to he need, and the many social, climatic, procurement and logistic needs.

Practically there is a considerable variation in tent specifications, both between catalogues and those deployed in the field. The purpose of this page is to provide clear specification and technical guidance defined by CARE shelter specialist for tents acquisition.

- Information/Specification:

General Specifications

| Dimensions | Usable Floor Area | 16.00 m2 |
| --- | --- | --- |
|  | Central Height | 2.15 m |
|  | Wall Height | 0.90 m |
|  | Ridge Length | 4.00 m |
| Frame | Standing & Ridgepoles of 48 mm dia. |  |
| Material | Outer Tent | Inner Tent |
|  | 320 g/m2 cotton/polyester blend water proof & rot proof fabric | Two folds, outer fold of 320 g/m2 cotton / polyester blend water proof & rot proof fabric, inner fold of 170 g/m2 cotton fabric |
| Color | Outer Tent | Inner Tent |
|  | Natural with greenish tint. | Outer Fold - Natural with greenish tint. Inner Fold - Yellow. |
| Ground Sheet | Tie able bathtub ground sheet of PE fabric |  |
| Windows | 4 with easily operable flap covers |  |
| Accessories | All required tools and accessories for ready use. Hammer, steel pegs and assembly instructions |  |
| Shipping Information |  |  |
| Packing | Tent + Inner Tent + Accessories in one bundle |  |
| Weight | 83.00 Kg (approx) |  |
| Volume | 235 x 30 x 30 cm / 0.21 cbm (approx) |  |
| Load ability |  |  |
| Sr.# | Container | Tents. |
| 1 | Heigh Cubic | 300 |
| 2 | 40 Ft | 250 |
| 3 | 20 Ft | 125 |

- Photo:

Detailed Specification

| 4x4m Family Tent |  |  |
| --- | --- | --- |
| Frame | Poles 48mm DIA OD Galvanized steel tubes (1.5mm minimum, 2mm maximum wall thickness) with welded 48mm DIA Galvanized steel cap (material - 4mm steel plate) and welded 120mm Galvanized steel pin (material 12mm DIA steel bar) Second ridge pole to include Swaged steel tube to 42mm OD Plates M10 steel nut welded to 50mm ID Galvanized steel tube (wall thickness 2mm +/- 0.5mm) welded to 150mm DIA x 2mm solid steel plate Plate keys 30mm OD steel ring welded to M10 x 30mm steel bolt |  |
| Accessories | 1 Hammer, 36 steel pegs & assembly instructions |  |
| Stitching | Lockstitch, 4-5 stitches per inch Thread - Polyester/Cotton core spun Sizes - Metric 36 Breaking Strength - 3.6kg min Construction - 3 ply, each yarn produced by spinning a sheath of cotton around a core of continuous filament polyester Finish - Type - SATIN starch & wax mixture |  |
| Ground Sheet | Material - Woven high-density polyethylene (HDPE) black fibres fabric laminated on both sides with low-density polyethylene (LDPE) coating. Reinforced with 6 bands of 7.5cm width made of woven black HDPE fibres fabric and coated outside. Position of bands as per drawing attached. Eyelets - Brass 12mm Internal Diameter. Located in the reinforcing bands to fit the toggle locations on the tent walls. Tensile Strength - Minimum 50DaN and 15% to 25% elongation in warp and weft under outside of reinforcement bands under ISO 1421. Minimum 70DaN inside of reinforcement bands as per ISO 1421 plus the additional procedure. Tear Strength - Minimum 10DaN under ISO 4674 (A") outside of the reinforcement bands. Welding - Maximum of two welds allowed, sheets should be of equal width, welding should be length wise. Minimum resistance is 80% of the original tarpaulin tensile strength in weft under ISO 1421 plus additional procedure. UV Resistance - Maximum 5% loss on original tarpaulin tensile strength under ISO 1421 after 1500 hours under ASTM G53/94 (UVB 313 nm peak), to be tested outside and inside of reinforcement bands. Weight - 170-200g/m2 +/- 5% to IFRC specifications and testing Temperature Resistance -20 to +80 degrees Celsius Features - Water, rot soil and fauna resistant. Long outdoor use life in all climates. Flammability - Flash point above 200 degrees Celsius Color - White sun reflective both sides, grey bands. Inner black fibers to ensure opacity. Printing - For each sheet, Manufacturer name, month and year of production (Letters of 2.5cm (1 inch) high maximum). One length indicator mark every meter. Webbing - 12mm wide filament polyester Weight - 10-12g per M Breaking Strength - 350 - 400 kg Thickness - 0.4 - 0.6mm Finish - Heat Set Color – Black. Heat seal all cut edges with hot knife |  |
| Outer Flysheet | Canvas - 50% cotton 50% Polyester ring spinning yarn count 10/2 x 10/2 twisted in warp 46/48 x weft 26/28 threads/square inch plain weave Weight - In loom state 270gsm (8oz per square yard) Finished weight 320gsm (9.4oz per square yard) Color - Natural (acceptable with slight greenish tint due to rot proofing) without objectionable spots/stains Waterproofing - To withstand 20cm hydrostatic head. Resistance to water penetration by paraffin emulsion and alum acetate Tensile Strength - Warp and Weft 85kgf Rot Proofing - Copper Naphtante or any appropriate agent Minimum 0.35% of dry weight of proofed canvas Width - 92cm (3ft) D rings Galvanized steel D ring 50mm x 30mm x 6mm, 15mm Dia ID Reinforcement Rings Galvanized steel ring insert hand stitched Ropes 6mm DIA polypropylene UV resistant Cut Length - 4M Construction - 3 Strand twisted Weight - 17g per M. Breaking Strength - 600 kg Color - Black. Heat seal all cut ends with hot knife |  |
| Inner Flysheet | Canvas - 50% cotton 50% Polyester ring spinning yarn count 10/2 x 10/2 twisted in warp 46/48 x weft 26/28 threads/square inch plain weave Weight - In loom state 270gsm (8oz per square yard) Finished weight 320gsm (9.4oz per square yard) Color - Natural (acceptable with slight greenish tint due to rot proofing) without objectionable spots/stains Waterproofing - To withstand 20cm hydrostatic head. Resistance to water penetration by paraffin emulsion and alum acetate Tensile Strength - Warp and Weft 85kgf Rot Proofing - Copper Naphtante or any appropriate agent Minimum 0.35% of dry weight of proofed canvas Width - 92cm (3ft) Lining (Dosouti) - 100% Cotton yarn count 20x20 in warp & weft 32 threads per inch in warp and weft 2x2 weave Weight - 170 gsm (6oz per square yard) Color - Dyed yellow. Uniform color-fast to water. No objectionable stains/spots Width - 92cm (3ft) Lacing Cord - 6mm DIA braided polyester cord UV resistant. Construction - Tandem / 8 plait Weight - 21 g per M. Breaking Strength - 560 kg Color – Black. Heat seal all cut ends with hot knife Webbing Ties - 25mm wide filament polyester Weight - 25 -30g per M Breaking Strength - 600 - 800 kg Thickness - 0.8 - 1.1mm Finish - Heat set. Color - Black Heat seal all cut edges with hot knife ID Mark - 297mm x 210mm PVC clear window pocket opening at top Thickness - 0.5mm Tensile strength - warp - 190kg /cm2, weft - 180kg /cm2 Tear Strength - warp - 6kg /mm, weft 6kg /mm Elongation - warp 240%, 260% Heat Shrinkage - warp Minus 5, weft plus 2 Weight - 640g /m2 Reinforcement rings 56mm Dia ID, Galvanized steel ring insert hand stitched Mud Flap PVC Coated Polyester Fabric - 160-170 gsm woven polyester yarn 1100 detex Coating - PVC on both sides weight - 340-440 gsm Weight - 500-610 gsm Adhesion - 60-80 N/5cm, DIN 53357, BS 3424/9B Tear Strength - Warp 300-400 N, Weft 200-350 N BS 3424/7B, DIN 53354 Tensile Strength - Warp 2000-225 N/5cm, Weft 1500-1800 N/5cm BS 3422/6A, DIN 53354 Temperature Resistance - 30 C to + 70 C, BS 3424/10 DIN 53372 |  |
| Windows | Window Mesh Yarn - 75 denier Multifilament: 36 filament 100% polyester ISO 2060, ISO 1833 Mesh - 25 holes/cm2; or 161 holes/inch2 (or minimum 156 holes/inch2) Weight - 75 denier: 30 g/m2 +/- 10% ISO 3801 Bursting Strength - 75 denier, min. 250 kPa 13938-2 (1999), head area = 7.3 cm2 Fabrication - Warp knitting ISO 8388 Dimensional Stability - Shrinkage +/- 5% ISO 3759 (1994) ISO 6330 (2000) - 8A, flat drying ISO 5077 (1984), Fire Safety - 16, CFR 1610 Fixing 25mm Velcro Webbing 12mm polyester |  |
| Partition | Sewn-in tabs in roof suitable for attaching an internal privacy wall |  |
| Ventilators | Fixing 25mm Velcro Webbing 12mm polyester |  |
| Pegs | Galvanized steel peg Remove all sharp edges on notches |  |
| Additional Information | Packing | Tent + Inner Tent + Accessories in one bale |
|  | Dimensions | 225 x 25 x 25 cm / 0.140 cbm (approx) |

- Pre-supply agreement: No

- Ind. Cost: +\- USD 280.00

- Vendor: Contact the HQ Procurement Unit for any information on this product

- Observations & Suggestions:

For additional info please check on

http://www.plastic-sheeting.org/ref/tents.pdf

http://www.shelterproject.org/downloads/spreports/techspecs.pdf

- Included full accessories

- Optional LOGO Mark printing