403 - Bladder Tank/Lay flat Tank/Pillow Tank

Return to catalog

- Usage:

These water bladder tanks, often referred to as lay flat or pillow tanks, have been developed especially for the harsh emergency aid environment.  There are two specifications, one for economic water storage and the second for heavy duty multi-site storage applications, water transportation and water distribution.

The tanks can be unrolled and used on any area of flat ground which has been cleared of debris.

- Information/Specification:

| Capacity | Tank Layflat Size | Groundsheet size | Tank Approx. Size Filled |
| --- | --- | --- | --- |
| 1,000 litres | 1.50 x 2.60 | 2.50 x 4.00 | 1.00 x 2.10 x 0.50 |
| 2,000 litres | 2.30 x 2.60 | 3.50 x 4.00 | 1.70 x 2.00 x 0.60 |
| 3,000 litres | 3.10 x 2.60 | 4.00 x 4.00 | 2.50 x 2.00 x 0.60 |
| 5,000 litres | 4.50 x 2.60 | 5.50 x 4.00 | 3.80 x 1.90 x 0.70 |
| 10,000 litres | 3.40 x 5.20 | 4.50 x 6.00 | 2.40 x 4.20 x 1.00 |
| 15,000 litres | 4.50 x 5.20 | 5.50 x 6.00 | 3.40 x 4.10 x 1.10 |
| 20,000 litres | 5.40 x 5.20 | 6.00 x 6.00 | 4.20 x 4.00 x 1.20 |
| 30,000 litres | 7.20 x 5.20 | 8.50 x 6.00 | 5.90 x 3.90 x 1.30 |
| 50,000 litres | 8.30 x 6.50 | 9.30 x 7.50 | 6.80 x 5.00 x 1.50 |

Bladder Material

| Properties | Specification |
| --- | --- |
| Base cloth | PES / PES |
| Total weight (approx.) | 1100 g/m² |
| Base cloth construction | Panama 2/2 275 g/m² |
| Construction | 12/13 threads/cm |
| Coating calender | Dull |
| Breaking strength | 4000 N / 5cm |
| Tear strength | 600 N |
| Adhesion | 90 N/5cm |
| Temperature resistance | -30° to +70° C |
| Colour | Beige 46002 |
| Special properties | Special quality for contact with potable water and food |

- Bladder Construction Detail

All bladders are fitted with reinforced corner mouldings with integral tie down holes.

All bladders are fitted with automatic pressure relief valves set at 1 PSI (0.007 N m/m²) to prevent bursting through over-filling.

| Lightweight top outlet with integral pressure relief valve | Heavy duty 4" top outlet with integral pressure relief valve |
| --- | --- |

Static use water tank outlets:-

1 x 2" BSP(M) reinforced PP moulded outlet with screw cap installed to one side of the tank.
1 x 4" BSP(M) PP moulded outlet with PVC screwed cap and integral pressure relief valve installed at the top of the tank.

Heavy duty static and transport use water tank outlets:-
2 x 2" BSP(F) anodised aluminium screwed outlets installed to one side of the tank.
1 x 4" BSP(F) anodised aluminium screwed outlet with PP screwed plug with integral pressure relief valve installed at the top of the tank.

General
All bladders are supplied with instruction manuals and repair kits. Tanks can be supplied with outlet valves pipe work or as kits with supply pumps and/or tap stands

Groundsheets
produced approximately 1m larger than the bladder tank dimensions when empty. All groundsheets are fitted with moulded in edge eyelets for pegging them down if required.

- Photo:

- Pre-supply agreement: No

- Ind.Cost:

- Bladder: 	5000 liters: 	1000 USD

10000 liters: 	1500 USD

15000 liters: 	2000 USD

- Vendor: Contact the HQ Procurement Unit for any information on this product

- - Observations & Suggestions:

Return to catalog