202 – MOSQUITO NET

- Return to catalog

- Usage:

Malaria is a major health problem; when planning a food /Non Food Items distribution, mosquito nets may be either linked to malaria prevalence within geographical areas or to the planned targeting of beneficiaries (groups within the population, refugee or IDP camps, large populations, etc).

- Information/Specification:

- PermaNet® 2.0 Brochure (English)

| Item | Requirement | Test Standard |
| --- | --- | --- |
| Efficiency |  |  |
| Insecticidal Effect | Net material must conserve >80 % functional mortality after 20 washes | SOP 003 SAL 01SOP.B.02 |
| Active Ingredient | Target Deltamethrin concentration is 55 mg/m2 ± 25% (lower limit is 45mg/m2).After 6 standard laboratory washes (as described in SOP.C.03) the concentration of Deltamethrin must be min 25 mg/m2 | SOP.C.01 SOP.C.03 |
| LN Technology | The net material is treated with Deltamethrin and a binding chemical to ensure the wash resistance of the insecticide. This is done on the net-material in a continuous industrial process to ensure even distribution of Deltamethrin |  |
| Net Material |  |  |
| Yarn | 75 or 100 denier Multifilament: 36 filaments 100 % polyester | ISO 2060 ISO 1833 |
| Mesh | 25 holes/cm2; or 161 holes/ inch2 (or minimum 156 holes/inch2) |  |
| Weight | 75 denier: 30 g/m2 ± 10%; 100 denier: 40 g/m2 ± 10 % | ISO 3801 |
| Bursting Strength | 75 denier, min. 250 kPa; 100 denier, min. 350 kPa | 13938-2 (1999), head area = 7.3 cm2 |
| Fabrication | Warp knitting | ISO 8388 |
| Dimensional Stability | Shrinkage ± 5% | ISO 3759 (1994) ISO 6330 (2000) - 8A, flat drying ISO 5077 (1984) |
| Fire Safety | 16 | CFR 1610 |
| Knitting Quality | No holes in net material or seams |  |
| Seam | Sewn using 100 % polyester thread |  |
| Seam Strength | 75 denier, min. 250 kPa, 100 denier, min. 350 kPa | 13938-2 (1999), head area = 7.3 cm2 |
| Dimension and Accessories | Refer to Shapes and Sizes |  |
| Standard colours | WH (White), LC1 (Yellow), LC2 (Pink), LC3 (Khaki), LC4 (Blue), DC1 (Dark Blue), DC2 (Dark Green-A), DC3 (Dark Green-B), DC4 (Green Madagascar), DC5 (Light Brown) as per the Colour Catalogue |  |

- Photo:

- Pre-supply agreement: No

- Cost: +\-10 USD

- Vendor: : Contact the HQ Procurement Unit for any information on this product

- Observations & Suggestions:

- The distribution of mosquito nets has to respect the intervention criteria defined by W.H.O. Explanation of the use and efficiency of mosquito nets to the beneficiaries have to be simple; saying that mosquito nets kill the mosquitoes and insects is much more efficient than a long speech on malaria disease. Any mosquito net distribution has to be followed by a monitoring process which includes their acceptance, understanding and correct use by the beneficiaries.

- There are different types of material (cotton, polyester, nylon, polyethylene,). We recommend polyester (PES) for all standard mosquito-nets. PES is a strong, low cost material easy to impregnate, widely available. - Specifications for material given here conform to the recommendation of WHO/Roll Back Malaria partnership (www.rbm.who.int ).

- In certain places, the usual mesh size is too big to protect efficiently (i.e.: against sandflies), check before ordering the protection required.

- All types of Mosquito nets should be provided with necessary straps and loops (or metal rings). Alternative sizes and colors can be procured as well. All nets are packed in plastic or nylon bags and carry an instruction leaflet.

Return to catalog