301 – PLASTIC SHEETING

- Return to catalog

- Usage:

Plastic sheeting (also known as plastic tarpaulin, tarp or polythene sheet) is a sheet of strong, flexible, water resistant or waterproof material. Although different qualities exist, those suitable for humanitarian relief are made from polyethylene. A standard sheet has a black woven or braided core and is laminated on both sides. Plastic sheeting is primarily used in construction for family shelter, sanitation or infrastructure projects, although it has many other uses.

- Information/Specification:

| Minimum specification: 190g/m2 Rolls and sheets |  |  |
| --- | --- | --- |
| Basic specification: |  |  |
| Weight | 190g/m2 ± 10% (ISO 3801). Add 10% for reinforcement. (Lighter versions that meet the material performance specifications below might also be considered) |  |
| Woven fabric | HDPE, BLACK colour (Black colour provides privacy and reduces heating under the sheeting due to the sun). |  |
| Lamination material | LDPE, WHITE colour on at least one side. (White colour reflects heat better in hot climates). |  |
| Reinforcement bands and eyelets (sheets only) |  |  |
| Reinforcement bands | 6 Grey bands of 7.5cm width made from black woven HDPE, laminated with LDPE, on both sides. |  |
| Sealed edges (with eyelets) | One strong aluminium eyelet every 1.00m ± 5% on edges. Sealed on all sides (or 2 sides heat sealed and two sides double stitched), with nylon or HDPE ropes in hem. |  |
| Material specification: |  |  |
| Tensile strength | Outside of reinforcement bands: Minimum 500N (ISO 1421) or Minimum 600N (BS 2576 50mm grab test) (US equivalent test ASTM D751) (For reinforced tarpaulin only: Inside of reinforcement bands: Minimum 700N (ISO1421) ) |  |
| Tear strength | Outside of reinforcement bands: Minimum 100N (under ISO 1421) (or BS 4303 wing tear). |  |
| Bursting strength | Not necessarily specified. (200N/cm2 (BS 4768)). |  |
| Welding | Maximum 1 welding along the middle. Minimum 80% of the original tarpaulin strength in the weft. (This means that sheets / rolls are made from two panels). |  |
| UV resistance | Maximum 5% loss on original tarpaulin tensile strength (ISO 1421) after a minimum of 1500 hours UV under ASTM G53/94 (UVB 313 nm peak). |  |
| Temp resistance | -20 to 800C where defined. (This is not necessary to define as HDPE/LDPE perform well within this temperature range) |  |
| Fire resistance | Ideally treated with fire retardant (CPAI 84-1995 section 6 >2000C). |  |

- Photo:

- Pre-supply agreement: No

- Cost: 	Tarpaulin 4x6m: +\- 18 USD\Pc

Plastic sheeting Roll 4x60m: +\- 150USD\roll

- Vendor: http://www.reltex.net

| Reltex Relief Supplies Ltd. Canvas Works Cox Lane, Chessington Surrey, KT9 1SG United Kingdom Tel: +44 (0) 20 8397 4373 Fax: +44 (0) 20 8397 4419 | Reltex Korea Ltd. 20-10, Nonhyun-Dong Kangnam-Ku, Seoul, Korea Tel: +82 2 543 0223 Fax 1: +82 2 543 2206 Fax 2: +82 2 548 1392 Mobile: +82 11 794 0223 | Reltex Relief Supplies, Inc. 3904 Darlington Avenue, N.W. Canton, Ohio 44708, U.S.A. Tel: +1 330 477 8130 Fax: +1 330 477 9130 | Reltex East Africa Ltd. 13 Salama Springs Old Portbell Road PO Box 11255 Kampala, Uganda Tel/Fax: +256 41 505 960 Mobile: +256 756 48641 |
| --- | --- | --- | --- |

- Distribution Network:

- Observations & Suggestions:

| Sheets 4mx6m or 5mx6m sheets with eyelets. 2400 sheets / 20' container (with palettes) 5400 sheets / 40' container (with palettes) | Rolls 60mx4m rolls 250 rolls / 20' container (with palettes) 550 rolls / 40' container (with palettes) |
| --- | --- |

- Return to catalog